## Slide 1: Minimization strategies in ptychography
Adaptative step length

## Slide 2: Outline
Minimization strategies theory
  Code to calculate and adaptative step length for object correction and angular positions correction
Application to simulated data

## Slide 3: Bragg Coherent Diffraction Imaging (BCDI)
Geometry of the experiment and rocking curve scan

## Slide 4: Introduction
Sample and experiment
Incoming beam
Outgoing beam
Detector

## Slide 5: Introduction:
A rocking scan allows to explore the shape of a Bragg reflection in 3D to retrieve information about the strain field, dislocations and defects in a crystalline sample
It is essential to control the angular position of the sample with respect to the incoming/outgoing beam
How can we correct and use the data, if there is some incertitude about the value of these angles which have been scanned?

## Slide 6: Theory of adaptive step to improve BCDI
Improving steepest descent algorithms and application to the rocking curve scan angles

## Slide 7: Steepest descent method
Is a category within the general line search method
The goal is to find the value of the variable x* which minimizes a certain function f(x):
We use the Taylor expansion of f(x) to explore its behavior in the vicinity of x_0 (initial value of the variable x) and to decide the new step: x_0+𝛅x

## Slide 8: Steepest descent method
How to calculate the step? if x* = x_0+𝛅x is a minimizer, then:

## Slide 9: Steepest descent method
In the case of a BCDI experiment, the function that we want to minimize is the error metric defined as:
Calculated intensity:
Calculated diffracted wave:
Measured
intensity

## Slide 10: Steepest descent method
Therefore we need to calculate the step which brings us from:
Applying the formula derived from the definition of minimizer and the Taylor expansion of the error metric function around \theta_{\hat{j}}, we obtain:

## Slide 11: Beyond the steepest descent: Minimization strategies theory
Adaptive step length theory (Marc Allain):
  Step beyond the Newton method where the step taken along variable x to minimize the function f(x) is given by:
  The Newton approach is inconvenient whenever we are far away from the minimum of f(x) at x_0, because f(x) is no longer well approximated by:

## Slide 12: Minimization strategies theory
Adaptive step-length theory (Marc Allain):
  We need a new approach… to take from Marc’s note

## Slide 13: Application of adaptative step to simulated data
Series of test on the rho and theta corrections

## Slide 14: Rho retrieval
Non distorted grid, perfect initial guess and noisy data

## Slide 15: Theta retrieval
Non distorted grid, perfect initial guess and noisy data
/…/Nanowire_ptychograpy/Irene_analysis/Theta_adaptative_step/results/NW_results_angle test
Object
Error metric
Angles
iterations
iterations

## Slide 16: Theta retrieval
Non distorted grid, perfect initial guess and noisy data

## Slide 17: Theta retrieval
Distorted grid, perfect initial guess of rho, but wrong initial guess of angles and non-noisy data

## Slide 18: Theta retrieval
Evolution of the angle value at different positions of the rocking curve
Rocking angle, theta

## Slide 19: Theta retrieval: correcting the rocking curve
Rocking angle
Rocking angle
40 Iterations

## Slide 20: Theta and rho retrieval
Perfect initial guess but distorted angles.
Rho and theta algorithm

## Slide 21: Rocking curve correction